|  | UT TECHNIQUE SHEET | Document No: NDT-UT-787-001 Rev. C Revision: C Date: Dec 17, 2024. |
| --- | --- | --- |

|  | DOCUMENT SUMMARY |
| --- | --- |

| Customer | Boeing Commercial Airplanes | Purchase Order | PO-BCA-2024-15847 |
| --- | --- | --- | --- |
| Part Number | LG-787-CYL-001 | Part Name | Main Landing Gear Actuator Cylinder |
| Material | Aluminum | Material Spec | AMS 4045 / QQ-A-250/12 |
| Part Type | Tube | Drawing No | DWG-787-LG-2024-001 |
| Process Spec | AMS-STD-2154E | Acceptance Class | AA |
| Inspection Type | Immersion | Criticality | Very Stringent |

|  | PART SKETCH / DIMENSIONS |
| --- | --- |

Key Dimensions:  Thickness: 25.4 mm  |  Axial Width: 320.0 mm  |  Outer Diameter (OD): 152.4 mm  |  Inner Diameter (ID): 101.6 mm

|  | TABLE OF CONTENTS |
| --- | --- |

1. Part Information

2. Equipment

3. Scan Parameters

4. Acceptance Criteria

5. Scan Details & Directions

5.1 Scanning Directions

5.2 Technical Drawing

6. Documentation

7. Calibration / Reference Standard

7.1 FBH Table

7.2 Calibration Block Diagram

7.3 Angle Beam Calibration Block

8. Approvals & Signatures

Note: Page numbers may vary based on content.

|  | 1. PART INFORMATION |
| --- | --- |

| Parameter | Value |
| --- | --- |
| Part Number | LG-787-CYL-001 |
| Part Name | Main Landing Gear Actuator Cylinder |
| Material | Aluminum |
| Material Specification | AMS 4045 / QQ-A-250/12 |
| Part Type / Geometry | Tube |
| Drawing Number | DWG-787-LG-2024-001 |
| Heat Treatment | T6 Solution Heat Treated and Aged |

|  |  | Dimensions |
| --- | --- | --- |

| Thickness | 25.4 mm |
| --- | --- |
| Axial Width | 320.0 mm |
| Outer Diameter (OD) | 152.4 mm |
| Inner Diameter (ID) | 101.6 mm |
| Wall Thickness | 25.40 mm |
| Hollow Part | Yes |

|  |  | Material Properties |
| --- | --- | --- |

| Material Density | 2700 kg/m³ |
| --- | --- |

|  | 2. EQUIPMENT |
| --- | --- |

| Parameter | Value |
| --- | --- |
| Manufacturer | Olympus NDT |
| Model | OmniScan X3 64 |
| Serial Number | OSX3-2024-0847 |
| Software Version | 5.2.1 |

| Frequency | 2.25 MHz |
| --- | --- |
| Type | Immersion |
| Transducer Shape & Size | - |
| Element Diameter | 0.500 inches |
| Couplant | Deionized Water |
| Selection Notes | - |

|  |  | Performance Parameters |
| --- | --- | --- |

| Entry Surface Resolution | 0.080 inches |
| --- | --- |
| Back Surface Resolution | 0.040 inches |

|  |  | Phased Array Configuration |
| --- | --- | --- |

| Number of Elements | 64 |
| --- | --- |
| Element Pitch | 0.60 mm |
| Wedge Model | SA32-N55S |
| Wedge Type | Normal Incidence |
| Delay Line | Water Path |

|  | 3. SCAN PARAMETERS |
| --- | --- |

| Parameter | Value |
| --- | --- |
| Scan Method | Immersion |
| Technique | Conventional |
| Scan Type | Automated C-Scan |
| Scan Pattern | Raster |
| Coupling Method | immersion |

|  |  | Speed & Coverage |
| --- | --- | --- |

| Scan Speed | 150 mm/s |
| --- | --- |
| Scan Index | 50 % |
| Coverage | 100% |
| Water Path | 25.4 mm |

|  |  | Instrument Settings |
| --- | --- | --- |

| Pulse Repetition Rate (PRF) | 2000 Hz |
| --- | --- |

|  | 4. ACCEPTANCE CRITERIA |
| --- | --- |

ACCEPTANCE CLASS: AA (Very Stringent - Primary Structure)

| Single Discontinuity | 3/64" (1.2mm) FBH response |
| --- | --- |
| Multiple Discontinuities | 2/64" (0.8mm) FBH (centers <1" apart) |
| Linear Discontinuity | 2/64" (0.8mm) FBH, 1/2" max length |
| Back Reflection Loss | 50% |
| Noise Level | Alarm level (see 5.2.3) |

|  |  | Special Requirements |
| --- | --- | --- |

Zone 1 (0-6mm from surface): No indications > #2 FBH equivalent. 100% coverage mandatory.

|  |  | Standard Notes |
| --- | --- | --- |

For engine mounts, landing gear primary structure, rotor hubs

|  |  | Table 6 — Ultrasonic Classes — Notes |
| --- | --- | --- |

1/ Any discontinuity with an indication greater than the response from a reference flat-bottom hole or equivalent notch at the estimated discontinuity depth of the size given (inches diameter) is not acceptable.

2/ Multiple discontinuities with indications greater than the response from a reference flat-bottom hole or equivalent notch at the estimated discontinuity depth of the size given (inches diameter) are not acceptable if the centers of any two of these discontinuities are less than 1 inch apart. Not applicable to class C.

3/ Any discontinuity longer than the length given with indications greater than the response given (flat-bottom hole or equivalent notch response) is not acceptable. Not applicable to class C.

4/ Loss of back reflection greater than the percent given, when compared to non-defective material in a similar or like part, is not acceptable when this loss of back reflection is accompanied by an increase or decrease in noise signal (at least double the normal background noise signal) between the front and back surface. Applicable only to straight beam tests.

5/ When inspecting titanium to class AA, the multiple discontinuity separation shall be 1/4 inch.

6/ For class AAA single discontinuity, 50% of 2/64 = 25% of 3/64.

7/ For class AAA linear and multiple discontinuities, 1/64 or 25% of 2/64 = 10% of 3/64.

|  | 5. SCAN DETAILS & DIRECTIONS |
| --- | --- |

|  |  | Scan Directions Overview |
| --- | --- | --- |

| Dir. | Wave Mode | Angle | Freq. | Make | Probe/Size | Remarks |
| --- | --- | --- | --- | --- | --- | --- |
| C | Longitudinal | 0° | 5.0 MHz | Olympus | V309-SU | OD straight-beam raster for wall volume coverage |
| D | Shear | 45° | 5.0 MHz | Olympus | SA32-N55S | Circumferential shear, clockwise, 45 deg for axial-oriented reflectors |
| E | Shear | -45° | 5.0 MHz | Olympus | SA32-N55S | Circumferential shear, counter-clockwise, 45 deg |
| F | Shear | 45° | 5.0 MHz | Olympus | SA32-N55S | Axial shear from OD, lead +45 deg |
| G | Shear | -45° | 5.0 MHz | Olympus | SA32-N55S | Axial shear from OD, lead -45 deg |
| H | Longitudinal | 0° | 5.0 MHz | Olympus | V309-SU | ID straight-beam follow-up for bore cleanliness and near-ID confirmation |

|  |  | Probe Parameters |
| --- | --- | --- |

| Dir. | Part Number | Serial Number | Active Element | Bandwidth | Focus Size | Velocity | Near Field |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C | V309-SU-05 | PRB-AL-24017 | 12.7 mm | high | 12 mm focus at 25 mm depth | 6320 m/s | 31.90 mm |
| D | SA32-N55S | ANG-24017-CW | 12.7 mm | medium | 45 deg wedge | 3130 m/s | 64.41 mm |
| E | SA32-N55S | ANG-24017-CCW | 12.7 mm | medium | 45 deg wedge | 3130 m/s | 64.41 mm |
| F | SA32-N55S | ANG-24017-AX1 | 12.7 mm | medium | 45 deg wedge | 3130 m/s | 64.41 mm |
| G | SA32-N55S | ANG-24017-AX2 | 12.7 mm | medium | 45 deg wedge | 3130 m/s | 64.41 mm |
| H | V309-SU-05 | PRB-AL-24017 | 12.7 mm | high | 10 mm focus at ID wall | 6320 m/s | 31.90 mm |

|  |  | U.T Parameters |
| --- | --- | --- |

| Dir. | U.T Parameter | Range | Delay | Gate 1 | TCG |
| --- | --- | --- | --- | --- | --- |
| C | 300V square / 130ns / longitudinal | 80 | 4 | 4-30-20% | YES |
| D | SW 45 deg / TCG +6 dB | 110 | 8 | 10-40-30% | YES |
| E | SW 45 deg / reverse lead | 110 | 8 | 10-40-30% | YES |
| F | OD axial sweep / 45 deg | 105 | 10 | 12-38-30% | YES |
| G | OD axial sweep / reverse | 105 | 10 | 12-38-30% | YES |
| H | ID confirmation pass / 300V square | 80 | 3 | 3-28-20% | YES |

|  | 6. DOCUMENTATION |
| --- | --- |

|  |  | Inspector |
| --- | --- | --- |

| Inspector Name | Dr. Michael Chen |
| --- | --- |
| Certification Number | ASNT-TC-1A Level III |
| Level | Level III |
| Certifying Organization | ASNT |

|  |  | Customer & Document |
| --- | --- | --- |

| Customer Name | Boeing Commercial Airplanes |
| --- | --- |
| Purchase Order | PO-BCA-2024-15847 |
| Part Serial Number | SN-LG787-2024-0342 |
| Inspection Date | Dec 17, 2024 |
| Procedure Number | NDT-UT-787-001 Rev. C |
| Drawing Reference | DWG-787-LG-2024-001 Rev. B |
| Revision | C |

|  |  | Additional Notes |
| --- | --- | --- |

Critical flight safety component. Requires Level III review and customer witness point.

|  | 7. CALIBRATION / REFERENCE STANDARD |
| --- | --- |

| Parameter | Value |
| --- | --- |
| Standard/Block Type | Cylinder (Notched) |
| Reference Material | Aluminum 7075-T6 |
| Block Dimensions | Curve (ID 101.6 mm, OD 152.4 mm, Thickness 25.4 mm) |
| Block Serial Number | CAL-AL-7075-001 |
| Last Calibration Date | Nov 15, 2024 |
| Metal Travel Distance | 12.7 mm |

|  |  | Flat Bottom Holes (FBH) |
| --- | --- | --- |

| P/N | Δ Type | Ø FBH (inch) | Ø FBH (mm) | E (mm) | H (mm) |
| --- | --- | --- | --- | --- | --- |
| - | distance | 1/64 | 0.40 mm | 25.4 mm | 6.3 mm |
| - | dac | 3/64 | 1.19 mm | 25.4 mm | 12.7 mm |
| - | dac | 7/64 | 2.78 mm | 25.4 mm | 19.1 mm |

|  |  | Calibration Block Diagram |
| --- | --- | --- |

|  |  | Angle Beam Calibration Block |
| --- | --- | --- |

Shear Wave / Circumferential Inspection Reference Block

|  | TECHNICAL DRAWING |
| --- | --- |

|  | ASTM E2375 SCAN DIRECTIONS DIAGRAM |
| --- | --- |

Standard Practice for Ultrasonic Testing of Wrought Products - Tube

Reference: ASTM E2375-16 "Standard Practice for Ultrasonic Testing of Wrought Products"

|  | 8. APPROVALS & DOCUMENT CONTROL |
| --- | --- |

|  |  | Revision History |
| --- | --- | --- |

| Rev | Date | Description | Prepared By | Approved By | Sign |
| --- | --- | --- | --- | --- | --- |
| C | Dec 17, 2024 | Initial Release | Dr. Michael Chen |  |  |

|  |  | Approval Signatures |
| --- | --- | --- |

| Role | Name (Print) | Cert. Number | Date | Signature |
| --- | --- | --- | --- | --- |
| UT Inspector (Level II) | Dr. Michael Chen | ASNT-TC-1A Level III | Dec 17, 2024 |  |
| Level III Review |  |  | - |  |
| Quality Assurance |  |  |  |  |
| Customer Representative |  |  |  |  |

⚠️ NOTICE: This technique sheet requires Level III approval before use in production.

DOCUMENT CONTROL

This is a controlled document. Unauthorized reproduction, modification, or distribution is strictly prohibited.

Printed copies are uncontrolled unless stamped "CONTROLLED COPY" with a valid date.

Document generated: March 21, 2026 | Scan-Master v1.0